## Slide 1: Erosion Characteristics in a Composite BN-SiO2 Hall Effect Thruster Chamber Wall
Thomas Burton, Dr. Gregory B Thompson
The University of Alabama
Dr. Mitchell Walker, Dr. Julian Rimoli
Aaron M. Schinder, German Capuano
Georgia Institute of Technology
AFOSR- FA9550-11-1-0160
Program Managers:
Dr. Mitat Birkan, Dr. John Luginsland, and Dr. Ali Sayir

## Slide 2: Background -- Hall Effect Thrusters
Inner wall
Outer wall
Graphite Cathode
Anode
Channel
Plasma Flow
Magnets

## Slide 3
Wall Erosion
  Sputtering of wall material into plasma?
  Thermal degradation from thermal cycling?
  Implantation of ion species into wall material?
Background -- Wall Erosion in HET
Motivation:
  Identify mechanisms of erosion
  Surface topology alterations and influence on plasma stability
(need to develop a quantifiable description of how the surface evolves under plasma operation)
HET Wall Chamber material types
  High Purity BN
  Combat©M26
    60wt% BN - 40wt%SiO2

## Slide 4: Background -- Processing of M26
Monoliths produced by Saint Gobain Advanced Ceramics -- mixing and hot pressing
Sectioned and machined to consumer specification

## Slide 5
5 μm
5 μm
5 μm
Low Erosion
Mild Erosion
High Erosion
Schematic of HET Discharge
UM/AFRL P5 HET*
  1.5 – 5 kW Operation
  2,000 hrs
  Xenon Plasma
Analysis -- Microstructural Erosion
*de Grys, Kristi. et all. “Demonstration of 10,400 Hours of Operation on a 4.5 kW Qualification Model Hall Thruster,”

## Slide 6: Analysis -- Phase Identification
No change in phase stability as function of eroded region
Amorphous silica
hcp BN
Silica (bright contrast) serves as a binding matrix with BN fibers (dark contrast)
10 μm

## Slide 7
Analysis -- 3D Serial Section of a BN Grain

## Slide 8
Analysis -- 3D Serial Section of a BN Grain
Serial sectioning was unable to be performed in the traditional manner using a Focused Ion Beam (FIB) system due to the non-conductive nature of the material. Instead, a traditional mounted sample was bisected allowing for two visible faces. The top face was repeatedly polished using 0.05um silica solution to act as the serial sectioning force. The side face had a reference mark milled into it using the FIB and the distance between the marker and the top faced used as the thickness for each serial section. Reconstructed was performed using the program Aviso Fire, and the resulting reconstruction suggests a BN platelet morphology, as would be expected from a graphite-like material.
5 μm
5 μm
5 μm
ROI
Serial sectioning

## Slide 9
5 μm
D
Analysis -- Highly-Eroded Region
Smooth planar silica surface –
BN micro-fiber exfoliation
Weak interphase bonding leading to grain exfoliation?
Surface protrusions –
Possible sputter erosion mechanism→ modeling underdevelopment
Secondary electron emission sites?
Micro-cracking prevalent in the BN phase
Exclusively along long axis of phase
Thermal expansion stresses?
Ion implantation stress (hcp BN versus more ‘open volume’ amorphous silica phase)?
Sputtering effects?
10 keV secondary electron SEM micrograph

## Slide 10
Analysis -- Topological Changes
Surface protrusions:
Comprise a laminate structure of BN and amorphous silica
Needle shape protrusions can be secondary electron emission source which influences plasma equilibrium with the wall material – future work
1mm

## Slide 11
Analysis -- Compositional Analysis of Surface Protrusions
Nitrogen
Silicon
Boron
Oxygen
1mm
100nm
1mm
1mm
Secondary Electron SEM micrograph
Back Scattered Electron SEM micrograph

## Slide 12
Analysis -- Chemical Analysis of Eroded Regions
X-ray Photospectroscopy (XPS):
  Preferential retention of silica in highly eroded region. In agreement with Garnier et al. "Low-Energy Xenon Ion Sputtering of Ceramics Investigated for Stationary Plasma Thrusters." J. of Vac. Sci. Tech. A 17. 6. 3246-3254 (1999).
1 μm
  Binding energy of BN > silica. Should expect slower sputter rate with BN…
BN exfoliation important mechanism for BN loss from the channel wall surface

## Slide 13
SEM micrograph – cracking most prevalent in BN, but some seen in silica
Analysis -- Micro-Cracking in Boron Nitride Phase
Phase identification confirmed amorphous silica and hcp BN
Prevalent and parallel micro-cracking in BN. Identified to be along the basal plane
Weak out-of-plane bonding (similar to graphite)
B, N
FIB extraction
TEM

## Slide 14
Analysis -- Investigation of Micro-cracking in Erosion Regions
1μm
Chart: Low Erosion Region
| 0 | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800 | 1900 | 2000 | More
 | 0 | 0 | 13 | 22 | 36 | 23 | 18 | 18 | 16 | 6 | 4 | 2 | 2 | 4 | 1 | 2 | 0 | 0 | 0 | 0 | 0 | 1
Average Crack Length: 535nm
Total Number of Cracks: 168/1400 mm2
Chart: Mild Erosion Region
| 0 | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800 | 1900 | 2000 | More
Frequency | 0 | 3 | 62 | 85 | 94 | 92 | 68 | 61 | 51 | 44 | 26 | 18 | 10 | 11 | 11 | 5 | 5 | 4 | 3 | 2 | 1 | 7
Average Crack Length: 589nm
Total Number of Cracks: 663/1400 mm2
Chart: High Erosion Region
| 0 | 100 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000 | 1100 | 1200 | 1300 | 1400 | 1500 | 1600 | 1700 | 1800 | 1900 | 2000 | More
Frequency | 0 | 18 | 145 | 172 | 150 | 94 | 81 | 61 | 49 | 40 | 26 | 24 | 15 | 16 | 12 | 3 | 4 | 4 | 2 | 0 | 3 | 8
Average Crack Length: 502nm
Total Number of Cracks: 927/1400 mm2
Conclusion: Increasing number of cracks with increasing erosion region suggests primary cracking mechanism to be nucleation of new cracks.
Red lines indicate measured cracks

## Slide 15
Analysis -- Thermally Induced Micro-Cracking – Finite Element Model
Simulation conditions:
  Anisotropic thermal expansion coefficient and elastic properties assigned to each boron nitride grain
  Silica phase assumed to be isotropic.
  Nominal temperature of 500K
Micrograph utilized for geometric representation
Basal-component of stress tensor for sample under thermal loading
Detail of tensile basal-component of stress tensor
Detail of compressive in-plane component of stress tensor
Preliminary results:
  Grains are found to experience tensile stresses on the order of 100s of MPa in the direction perpendicular to the basal plane while experiencing similar compressive stresses on the orthogonal direction
  This stress state could easily lead to the kind of micro-cracks observed.

## Slide 16
Conclusions
Identified three distinct features of plasma erosion microstructure
  Micro-cracking
  Surface protrusions
  Boron Nitride exfoliation
5 μm
Preferential Retention of SiO2 over Boron Nitride
  Suspected result of exfoliation
Crack nucleation in Boron Nitride source of micro-cracking
  Modelling suggests thermal expansion stress
  Future work with thermal cycling
Surface protrusions as sites for Secondary Electron Emission
  Future work quantifying effect of topology on electron emission